## Slide 1: Synthesis & Structure of Hexafluoridouranates(V)
Lena-Marie Aßmann, Timo Wolf
Supervised by: Jun. Prof. Dr. Suta
28th November 2025
Notes: Welcome to our presentation about the synthesis and structure of hexafluoridourantes(V)

## Slide 2: Where can I read about that?
What are Hexafluoridourantes(V)?
How to synthesize these compounds?
What is the structure of these compounds and
how are the structures connected?
[1] B. Scheibe, T. B. Wassermann, F. Kraus, Inorg. Chem. 2025, 64, 18432–18446.
Notes: These talk is based on a paper by these people which was published this year in the journal Inorganic chemistry. After reading the paper you can answer what hexafluoridourantes(V) are, how these compounds can be synthesized and how the structure of these compounds is and how they are connected to each other. For this they using a lot of rather advanced crystallography

## Slide 3: Concepts / Methods
Working with anhydrous HF
Uranium-chemistry
Notes: At first i will talk a little bit about the methods that are used to synthesize the desired compounds, because they are rather exotic. Lets start with working with anhydrous hydrogen fluoride

## Slide 4: Working with anhydrous HF
HF is very toxic!
Glass vessels can‘t be used!
Passivation & baking out is needed!
Notes: Hydrogen fluorid and the solution in water called hydrofluoric acid are very toxic and i mean really toxic. The fluorid ions cause the precipation of calcium and magnesium fluoride, which leads to a disturbance of the electrolyte balance in the body. This is often toxic.
Because hydrogen fluorid is one of the only compounds that react with glass you cannot use normal glas ware. Glass can be discribed as silcium dioxide. 4 equivilents of hydrogen fluorid react with silicium dioxide to siliciumtetrafluoride and water. Therefore the schlenk line used is made out of monel, which is a copper-nickel-alloy. The used schlenk tubes are made out of PFA witch is a fluoropolymer.
Before working with this fluoropolymer the reaction vessels were baked out to remove any water. Anhydrous hydrogenfluorid is miscible in any ration with water. The reaction vessels and the schlenk line also need to be passivated before use to make sure nothing gets damadged.

## Slide 5: Concepts / Methods
Working with anhydrous HF
Uranium-chemistry
[II]
Notes: Uranium compounds are also used, although this has become rather uncommon in modern days

## Slide 6: Alkali metals

## Slide 7: Synthesis of alkali metal Hexafluoridouranates(V) MUF6
Synthesis of β-UF5:
Properties: tetragonal symmetry, (No. 122)
Synthesis of MUF6:
M = Li - Cs

## Slide 8: Structural chemistry of LiUF6
trigonal
(No. 148)

## Slide 9: Structural chemistry of NaUF6 & CsUF6
trigonal
(No. 148)
 | LiUF6 | NaUF6 | CsUF6
a [Å] | 5.1902 | 5.4101 | 8.0284
b [Å] | 14.265 | 15.746 | 8.4388
V [Å3] | 332.78 | 399.12 | 471.05
V/Z [Å3] | 110.93 | 133.04 | 157.02
 | LiUF6 | NaUF6 | CsUF6
d(U-F) [Å] | 2.0624 | 2.0661 | 2.057
d(M-F) [Å] | 2.0061 | 2.2768 | 
d(U-U) [Å] | 5.1902 | 6.1078 | 5.1732

## Slide 10: Structural chemistry of KUF6
monoclinic
(No. 12)

## Slide 11: Structural chemistry of RbUF6
monoclinic
(No. 12)
 | KUF6 | RbUF6
d(U(1)-F(1)) [Å] | 2.0633 | 2.0600
d(U(1)-F(2)) [Å] | 2.0635 | 2.0573
d(U(1)-F(3)) [Å] | 2.3400 | 2.3286
d(U(1)-F(4)) [Å] | 2.3403 | 2.3286
d(U(1)-U(1)#1) [Å] | 4.0102 | 4.0019
d(U(1)-U(1)#2) [Å] | 4.0243 | 4.0148
 | KUF6 | RbUF6
a [Å] | 11.442 | 11.797
b [Å] | 8.0345 | 8.0167
c [Å] | 5.5655 | 5.7272
β [°] | 90.128 | 90.00
V [Å3] | 511.62 | 541.64
V/Z [Å3] | 127.905 | 135.41

## Slide 12: Usage of alkali metal analogus
AgUF6
TlUF6
Solid-state reaction
Preparation in solution
Byproduct of a reaction
Isotypic to KUF6!
But: Shorter U-F-bond length, shorter U-U-distances
tetragonal
P42/m (No. 84)
monoclinic
(No. 12)
Notes: In addition the group used other metalfluorides like thalliumfluorid which can be described as an alkali metal analog.
There are two ways to synthesis thalliumhexafluoridouranat(5). One is a solid state reaction, the equation is shown here. The other possibility is the preparation of the desired in solution just like all the other compounds. For this case the reaction is shown here.
When it comes to the structural chemistry of TlUF6 it is shown that TlUF6 is isotypic to KUF6, which means it crystallizes in the same space group type. The coordination number of uranium is 8, the coordination polyeder is a distorted trig. Dodecahedron. The coordination number of thallium is 10, the correspondening coordination number is a distorted pentagonal prisma.
In comparision with KUF6 and RbUF6 the Uranium-Fluor-bond length is the shortest. This is due to the larger effectiv ionic radius of the thallium ion. That can be also seen at the shorter Uranium-Uranium distance.
Warum ist Tl+1 stabiler als Tl3+? Inert Pair Effekt bei schweren Hauptgruppenelementen, d-Orbitale sind diffuser und können die zunehmend effektivere kernladung nicht kompensieren, daher werden die s-Orbitale immer inerten, weil sie näher an den Kern gezogen werden. Es ist schwerer die Elektronen aus diesen Orbitalen zu entfernen.
TlUF5 ist isotyp zu KUF6 , also ebenfalls monoklines Kristallsystem, KZ = 8 Uran, Koordinationspolyeder ist verzerrtes trigonales Dodecaeder, Tl+ ist mit zehn Fluoridatomen koordiniert, Koordinationspolyeder ist also

## Slide 13: Relationship AgUF6 & KUF6

## Slide 14: Synthesis of H3OUF6
Structural chemistry
Cubic
Ia (No. 206)
How to use water without usage of water?
[1] B. Scheibe, T. B. Wassermann, F. Kraus, Inorg. Chem. 2025, 64, 18432–18446. Supporting Information

## Slide 15
Structural chemistry
[7] U. Müller, Anorganische Strukturchemie, Vieweg & Teubner, 2008.

## Slide 16: Synthesis of Ba[U2F12]·1.36 HF
orthorhombic
Pnma (No. 62)
Structural chemistry
Similar to the previous synthesis of Sr[U2F12]

## Slide 17: Thank you for listening. Are there any questions?

## Slide 18: What is good & what is bad?
Unusual topic and synthesis methods
A lot of different structures
Nicely written & understandable without expertise
Structure of cubic NaUF6?
More information on CsUF6?
What’s about other earth alkali metal U2F12 compounds?

## Slide 19: If we have sparked your interest:
The Most Dangerous Chemical Reaction – Fluorine Meets Cesium
by Advanced Tinkering
FluorLab
by Advanced Tinkering
Videos about and with Florian Kraus & his group
Everything you ever wanted to know about the production and purification of alkali metals
by Advanced Tinkering
Wie GEFÄHRLICH ist Fluor? Das REAKTIVSTE Element der Welt!
by Elias Experiments
Or short videos by Florian Kraus himself! @FluorineIsGreat

## Slide 20: Comparison of the structural data
 | LiUF6 | NaUF6 | CsUF6
crystal system | trigonal | trigonal | trigonal
space group | R-3 | R-3 | R-3
Z | 3 | 3 | 3
a [Å] | 5.1902 | 5.4101 | 8.0284
b [Å] | 14.265 | 15.746 | 8.4388
V [Å3] | 332.78 | 399.12 | 471.05
V/Z [Å3] | 110.93 | 133.04 | 157.02
 | LiUF6 | NaUF6 | CsUF6
d(U-F) [Å] | 2.0624 | 2.0661 | 2.057
d(M-F) [Å] | 2.0061 | 2.2768 | 
d(U-U) [Å] | 5.1902 | 6.1078 | 5.1732

## Slide 21: Comparison of the structural data
 | KUF6 | RbUF6 | TlUF6
crystal system | monoclinic | monoclinic | monoclinic
space group | C2/m | C2/m | C2/m
Z | 4 | 4 | 4
a [Å] | 11.442 | 11.797 | 11.895
b [Å] | 8.0345 | 8.0167 | 7.9983
c [Å] | 5.5655 | 5.7272 | 5.6787
β [°] | 90.128 | 90.00 | 90.00
V [Å3] | 511.62 | 541.64 | 540.28
V/Z [Å3] | 127.905 | 135.41 | 135.07
 | KUF6 | RbUF6 | TlUF6
d(U(1)-F(1)) [Å] | 2.0633 | 2.0600 | 2.0538
d(U(1)-F(2)) [Å] | 2.0635 | 2.0573 | 2.0611
d(U(1)-F(3)) [Å] | 2.3400 | 2.3286 | 2.3241
d(U(1)-F(4)) [Å] | 2.3403 | 2.3286 | 2.3264
d(U(1)-U(1)#1) [Å] | 4.0102 | 4.0019 | 3.9937
d(U(1)-U(1)#2) [Å] | 4.0243 | 4.0148 | 4.0046
d(M(1)-F(1)) [Å] | 2.6995 | 2.833 | 2.8394
d(M(1)-F(1)) [Å] | 3.0950 | 3.1123 | 3.1410
d(M(1)-F(2)) [Å] | 2.6897 | 2.8308 | 2.8311
d(M(1)-F(2)) [Å] | 3.0902 | 3.1168 | 3.1485
d(M(1)-F(3)) [Å] | 2.6762 | 2.7691 | 2.7962
d(M(1)-F(4)) [Å] | 2.6886 | 2.7694 | 2.8052

## Slide 22: Structural field diagram